J30	LIQUID APPLIED TANKING / DAMP PROOFING

To be read with Preliminaries / General conditions.

EXECUTION  continued.

J30/261	JUNCTIONS WITH STRUCTURESEAL

- Apply 300mm wide band of RIW Sheetseal 226, lapped 150mm onto RIW Structureseal, and 150mm onto adjacent structure.

- Seal together using 50 x 5mm bead of RIW Sealing Compound, in centre of lap.

- Apply strip of RIW Universal Tape across end of RIW Sheetseal 226, which is to be coated with Flexiseal.

- Apply RIW Flexiseal, lapped over the RIW Sheetseal 226, by 200mm minimum.

- Do not apply RIW Flexiseal Primer onto RIW Sheetseal 226 or RIW Universal Tape.