J40	FLEXIBLE SHEET TANKING / DAMP PROOFING

To be read with Preliminaries / General conditions.

TYPES OF TANKING / DAMP PROOFING

J40/140  	LOOSE LAID POLYETHYLENE GAS RETARDANT DAMP PROOFING

- Substrate : …………………

-     Primer : Not required

- Manufacturer : RIW Limited, Arc House, Terrace Road South, Binfield, RG42 4PZ.

Tel : 01344  397777   Fax : 01344  862010

E-mail : technical@riw.co.uk     Web : www.riw.co.uk

-	Product reference : RIW Gas Seal Black.

- Colour : Black and white

- Number of layers : One.

- Thickness / Gauge : 0.6mm ( applied ).

- Laying : Overlapped with staggered joints

- Joints :

- Surfaces to be joined : Clean and dry beyond full width of joint.

- Laps ( minimum ) :150mm.

- Sealing : RIW Gas Tape HC, placed centrally in the lap.  RIW Lap Tape HB, laid over the edge of the upper sheet, by 50mm, and adhered on to the lower sheet.

- Accessories : See product data sheet.

WORKMANSHIP

J40/310	WORKMANSHIP GENERALLY

- Condition of substrate :

-	Clean and even textured, free from voids and sharp protrusions.

-	Moisture content : Compatible with damp proofing / tanking.

- Air and surface temperature : Do not apply sheets if below minimum recommended by membrane manufacturer.

- Condition of membrane at completion :

-	Neat, smooth and fully supported, dressed well into abutments and around intrusions.

-	Completely impervious and continuous.

-	Undamaged. Prevent puncturing during following work.

- Permanent overlying construction : Cover membrane as soon as possible.

J40/320	INSPECTION

- Give notice : Before covering any part of membrane with overlying construction.

- Independent validation and integrity testing required.

J40/360	JUNCTIONS WITH PROJECTING DPC’S / CAVITY TRAYS

- Adjoining surfaces : Clean and dry.

- Dpc’s / cavity trays : Lap and fully bond / seal with RIW Gas Tape HC.

-	Laps ( minimum ) : …………………

-	Bonding / Sealing : …………………

J40/370A	PIPES, DUCTS, CABLES ETC :

- Where these pass through sheeting, make junctions completely impervious using RIW Pre-formed Collars

- Adjoining surfaces : Clean and dry.

- 	Laps :

- Lap and fully bond / seal with RIW Gas Tape HC.