C42	REPAIRING / RENOVATING / CONSERVING  CONCRETE

To be read with Preliminaries / General conditions.

J40/310333333333

3100110101010293I8E4844444

310A	REPAIR MORTAR

- Type : Polymer modified cementitious mortar

- Manufacturer : RIW Ltd, 487/488 Ipswich Road, Slough, Berkshire SL1 4EQ

Tel : +44 1753 944200

E-mail : technical@riw.co.uk

Web : www.riw.co.uk

-     Product reference : RIW Cementfill FC

- Application thickness : 6mm maximum per layer.

- Primer : Not required

or : for highly porous substrates

- Primer : RIW Cementseal Primer

J40/310333333333

3100110101010293I8E4844444

320A	LEVELLING / SMOOTHING COATS

- Type : Polymer modified cementitious mortar

- Manufacturer : RIW Ltd, 487/488 Ipswich Road, Slough, Berkshire SL1 4EQ

Tel : +44 1753 944200

E-mail : technical@riw.co.uk

Web : www.riw.co.uk

-     Product reference : RIW Cementfill FC

- Application thickness : 0 to 6mm.

- Primer : Not required

or : for highly porous substrates

- Primer : RIW Cementseal Primer