M10 CEMENT BASED LEVELING / WEARING SCREEDS

To be read with Preliminaries / General conditions.

J40/310333333333

3100110101010293I8E4844444

140A PROPRIETARY POLYMER MODIFIED LEVELLING SCREEDS

* Substrate : …………………
* Manufacturer : RIW Ltd, 487/488 Ipswich Road, Slough, Berkshire SL1 4EQ

Tel : +44 1753 944200

E-mail : [technical@riw.co.uk](mailto:technical@riw.co.uk)

Web : [www.riw.co.uk](http://www.riw.co.uk)

- Product reference : RIW Cementfill FC

* Screed construction : Fully bonded.
* Thickness :

- Nominal : 3mm.

- Minimum : 0mm.

- Maximum : 6mm per layer.

* Mix :

- Proportions : 6.5 parts powder to 1 part water, by volume.

* Primer : RIW Cementseal Primer
* Finish : …………………

- To receive …………………

- Other requirements …………………