J31 LIQUID APPLIED WATERPROOF ROOF COATINGS

To be read with Preliminaries / General conditions.

**TYPES OF COATING ; Products**

J30/353 WATERPROOF COATING

- Type : Polymer modified epoxy coating

- Manufacturer : RIW Ltd, 487/488 Ipswich Road, Slough, Berkshire SL1 4EQ

Tel : +44 1753 944200

E-mail : [technical@riw.co.uk](mailto:technical@riw.co.uk)

Web : [www.riw.co.uk](http://www.riw.co.uk)

- Product reference : RIW Flexiseal Pro ; two-pack

- Primer : RIW Flexiseal Pro Primer ; two-pack

- Application : Number of coats : Primer - 1 coat minimum

Membrane - 1 No. Horizontally - 2 No. Vertical

* Coverage per coat (minimum) : Primer - 4m2 / litre

Membrane - 1 m² / kg Horizontal, 2 m2 / kg Vertical

- Reinforcement : Not required.

or

- Reinforcement : Embed Flexiseal Pro Scrim between two layers of Flexiseal Pro, laid wet on wet, where required / specified.

* Colour : Black primer, Red membrane
* Minimum dry film thickness : Primer - 220 microns / coat

Membrane – 880 microns