J31 LIQUID APPLIED WATERPROOF ROOF COATINGS

 To be read with Preliminaries / General conditions.

 **TYPES OF COATING ; Products**

J30/353 WATERPROOF COATING

 - Type : Polymer modified epoxy coating

 - Manufacturer : RIW Ltd, 487/488 Ipswich Road, Slough, Berkshire SL1 4EQ

 Tel : +44 1753 944200

 E-mail : technical@riw.co.uk

 Web : [www.riw.co.uk](http://www.riw.co.uk)

 - Product reference : RIW Flexiseal Pro ; two-pack

 - Primer : RIW Flexiseal Pro Primer ; two-pack

 - Application : Number of coats : Primer - 1 coat minimum

 Membrane - 1 No. Horizontally - 2 No. Vertical

* Coverage per coat (minimum) : Primer - 4m2 / litre

 Membrane - 1 m² / kg Horizontal, 2 m2 / kg Vertical

 - Reinforcement : Not required.

or

 - Reinforcement : Embed Flexiseal Pro Scrim between two layers of Flexiseal Pro, laid wet on wet, where required / specified.

* Colour : Black primer, Red membrane
* Minimum dry film thickness : Primer - 220 microns / coat

 Membrane – 880 microns