J31	LIQUID APPLIED WATERPROOF ROOF COATINGS

To be read with Preliminaries / General conditions.

TYPES  OF COATING ; Products

J30/353 	WATERPROOF COATING

-	Type : Polymer modified epoxy coating

-   	Manufacturer : RIW Limited, Arc House, Terrace Road South, Binfield, RG42 4PZ.

Tel : 01344  397777   Fax : 01344  862010

E-mail : technical@riw.co.uk   Web : www.riw.co.uk

- 	Product reference : RIW Flexiseal Pro ; two-pack

- 	Primer : RIW Flexiseal Pro Primer ; two-pack

-	Application : Number of coats : Primer - 1 coat mimnimum

Membrane  - 1 No. Horizontally - 2 No. Vertically

- Coverage per coat (minimum) : Primer - 4m2 / litre

Membrane - 1 m² / kg Horizontal, 2 m2 / kg Vertical

-	Reinforcement : Not required.

or

-	Reinforcement : Embed Flexiseal Pro Scrim between two layers of Flexiseal Pro, laid wet on wet, where required / specified.

- Colour : Black primer, Red membrane

- Minimum dry film thickness : Primer - 220 microns / coat

Membrane – 880 microns